| 项目名称 Project Name | Integrated Petrochemical Complex Construction in Atyrau Region | 报告号 Report No. | CAPTCC-CT1801725-IR-01 |
| --- | --- | --- | --- |
| 客户 Client | TCC | 客户订单号 Client P.O. No. | / |
| 检验通知号 Reference No. | / | 检验员 Inspector | Ma Junxu |
| 制造商 Vendor | Zhengzhou chengxin steel structure co. LTD | 检验地址 Inspection Location | Yuanyang county, xinxiang city, henan province |
| 分包商 Sub-Vendor | / | 检验日期 Visit Date(s) | 2020.01.01-05 |

| 本次检验参与人员 THE PARTICIPANTS OF THIS VISIT |
| --- |
| 姓名 NAME | 公司 COMPANY | 代表方 REPRESENTING | 联系方式 CONTACT NO. |
| Ma Junxu | CAPTCC | TCC | 18629353479 |
| Wang Shuliang | Chengxin steel structure | Vendor | 13523406589 |
| Fan Feng | Chengxin steel structure | Vendor | 13598085276 |

| 本次检验产品 MATERIAL/ SUBJECT OF INSPECTION | 编号 Item No. | 订单数量 QTY as per P/O | 所检数量 QTY offered for inspection |
| --- | --- | --- | --- |
| steel structure | About 2000T |

| 适用文件 参考附件 REFERENCE DOCUMENTATION Refer to attachments instead |
| --- |
| 标题 Title | 文件编号 Reference No | 版本 Rev. | 批准状态 Approval status | 批准人 Approved by | 日期 Date |
| QZKPI-0000-BS-SPC-0004_A03__Standard__for__Fireproofing__of__Structural__Steelworks | QZKPI-0000-BS-SPC-0004 | REV A02 | Acc. | / | 2019/9/2 |
| QZKPI-0000-MA-SPC-0007_A03 Specification for Protective Painting and Application Requirements (Native) -20190905 | QZKPI-0000-MA-SPC-0007 | REV A03 | Acc. | / | / |
| Meeting minutes fire coverage confirmation 8411-3 | / | / | Acc. | / | / |
| SPECIFICATION FOR STEEL STRUCTURE | / | / | Acc. | / | / |
| Steel structure drawing | / | / | Acc. | / | / |

| ITP 相关 REFERENCE ITP |
| --- |
| 序号 S/N | 设备名称 Equipment/material | 检验项目 Inspection Activity (detail according to scope /standard/etc.) | 检验等级 Inspection Level H/W/SW/R | 相关文件 Relevant document |
| / | / | / | / | / |

| 检验结果 INSPECTION RESULT |
| --- |
| 合格 Satisfactory (without comments) | 假释 Satisfactory with comments (Any of trailing punch or non-conformity items is still open) | 不合格 Not Satisfactory (NCR raised during the inspection) |
| 检验概述： SUMMARY According to the inspection notice (No. : task list -CNCEC kazakh project -025), the inspectors have Expediting and inspection of steel structures produced by zhengzhou chengxin steel structure co., LTD.Details of this week's inspection are as follows: Yuanyang factory: 266 Pcs of assembly completed, 102.562T, 8 Pcs of welding completed, 12T. The paint has not started yet. Qixain factory: 345 Pcs of assembly completed, 158.873T, 219 Pcs of welding completed, 81,303T, 215 Pcs of paint completed, 76.822T. All the straight pieces have been completed this time. Please see the attached list of steel structures for details. According to the paint regulations, Primer + intermediate + finish, it takes two days for one coat of paint to dry completely, and six days for three coats of paint. The factory has been asked to increase heating equipment as soon as possible. |
| 不符合项 Open Non Conformities： | 是，详见不符合项表格： Yes, details in non-conformities： | 无 No |
| 尾项清单： Open Punch List Items： | 是,详见尾项情单表格： Yes, details in punch list | 无 No |
| 检验员签名： Inspector signature： |  | 报告日期： Inspection report date： | 2020/01/06 |

| 不符合项 参考附件 NON CONFORMITIES Refer to attachments instead |
| --- |
| 项目 Item | 描述 Description | 状态 Status | 提出日期/报告号 Raised on/ Report # | 关闭日期/报告号 Closed on/ Report # | 备注 Comments |

| 尾项清单 参考附件 PUNCH LIST Refer to attachments instead |
| --- |
| 项目 Item | 描述 Description | 状态 Status | 提出日期/报告号 Raised on/ Report # | 关闭日期/报告号 Closed on/ Report # | 备注 Comments |
| 1 | Yuanyang and qixian factory factory has a total of 20 people in production, and the staff is seriously insufficient. | Closed on | 2020/01/05 | IR01 | 2020/01/05 | IR01 | It has increase to 40 people |
| 2 | The inspector randomly checked the Steel members No. AB3-37 and found that there were 3 places without welding. | Closed on | 2020/01/05 | IR01 | 2020/01/05 | IR01 | See photos |
| 3 | Inspectors randomly sampled the steel components and found that most of the components had serious appearance quality problems such as welding deviation, porosity, welding slag and spatter, edge bite, burr on the reinforced plate of the bottom plate, and misalignment. | Closed on | 2020/01/05 | IR01 | 2020/01/05 | IR01 | See photos |
| 4 | Steel members No. AC1-1/2 bottom plate bolt holes do not meet the requirements of the drawing, which requires 42mm, actual measurement 45mm. | Open | 2020/01/05 | IR01 |  |  |  |
| 5 | The inspectors found that most of the measuring instruments in the factory had no calibration certificate. | Open | 2020/01/05 | IR01 |  |  |  |
| 6 | The paint is short of color card, we have asked the factory to provide it as soon as possible. | Open | 2020/01/05 | IR01 |  |  |  |
| 7 | There is no testing equipment for steel structure roughness, so the factory has been required to rectify. | Open | 2020/01/05 | IR01 |  |  |  |

| 检验项目 THE ITEMS OF INSPECTION |
| --- |
| 预检会 Pre-inspection Meeting |  | 材料检验 Material Inspection |  | 数量检查 Quantity Check |  |
| 外观检验 Visual Inspection |  | 尺寸检验 Dimension Inspection |  | 试验见证 Test Witness |  |
| 防腐检验 Coating Inspection |  | 文件审核 Documents Review |  | 包装唛头检验 Packing & Shipping Mark Inspection |  |
| 装车/船检验 Loading Inspection |  | 铭牌/标记核对 Nameplates/Marking verification |  | 其他 Others |  |

检验详述 INSPECTION DETAILS

检验活动如下： Description of the inspections carried out: 1.材料检验MATERIALS INSPECTION According to the file(QZKPI-0000-MA-SPC-0007_A03 Specification for Protective Painting and Application Requirements (Native) -20190905)Inspectors checked the paint brands and found that they met specific brand requirements (Osakapaint). 2.数量检查QUANTITY CHECK The inspector checked the quantity against the steel structure list submitted by the factory and the result was acceptable.See steel structure production list. 外观检验VISUAL INSPECTION According to the drawings and the steel structure specification, the inspectors carried out random appearance inspection on the supports, steel beams and steel columns.Details are as follows: There are serious appearance quality problems such as welding deviation, blowhole, welding slag and spatter, edge bite, burr and misalignment in the bottom plate stiffened plate. The appearance of the steel structure paint has the problems of bead hanging and bruising and fold,Rectify before packaging. The inspector randomly checked the Steel members No. AB3-37 and found that there were 3 places without welding.has the rectification.See photos 4.尺寸检验DIMENTION INSPECTION According to the drawings, the inspectors randomly inspected the dimensions of supports, steel beams and steel columns in the production process. The details are as follows： The distance between the profile and the stiffener connection was checked. Connection plate hole spacing inspection. Steel members No. AC1-1/2 bottom plate bolt holes do not meet the requirements of the drawing, which requires 42mm, actual measurement 45mm.Waiting for factory rectification. 5.防腐检验COATING INSPECTION According to the paint regulations(QZKPI-0000-MA-SPC-0007_A03 Specification for Protective Painting and Application Requirements (Native) -20190905 and QZKPI-0000-BS-SPC-0004_A03__Standard__for__Fireproofing __of__Structural__Steelworks),Primer + intermediate + finish,The inspector inspected the primer and intermediate paint randomly. The details are as follows： There is no testing equipment for steel structure roughness, so the factory has been required to rectify. Primer + middle paint film thickness meets the requirements. Finish to be sprayed. 铭牌/标记核对NAMEPLATES/MARKING VERIFICATION N/A 7.包装和标识检验PACKING AND SHIPPING MARK INSPECTION The inspector has checked the marking of the steel structure. Each steel structure has a marking plate. The result is acceptable. Waiting for the packing. 装车/装船检验 LOADING INSPECTION N/A 9.放行RELEASE N/A 10.文件审查 DOCUMENTATION REVIE N/A

| 附件 ATTACHMENT |
| --- |
| 序号 Item | 附件名称 Attachment name | 描述 Description |
| 1 | CAPTCC-CT1801725-IR01-Photos | Photos |
| 2 | CAPTCC-CT1801725-IR01-Steel structure production list | Steel structure production list |
| 结束 End of Report |